AXC.32.02

KETJENFLEX® MH

Co-resin for overprint varnishes

General Information

KETJENFLEX® MH is a flexibilizing co-resin used in overprint varnishes.

Description and Application

KETJENFLEX® MH is typically used when a combination of flexibility and gloss of the overprint varnish is required. KETJENFLEX® MH is compatible most common ink resin systems like nitrocellulose, polyurethane, ketonic and vinyl based systems.

Though KETJENFLEX® MH is delivered in the form of a hard resin it will provide flexibility, toughness and durability to the system. KETJENFLEX® MH imparts improved adhesion and wear properties and generally provides the lacquer with a shiny glossy appearance.

Applications:

- Nitrocellulose based overprint varnish

- Nitrocellulose/Polyurethane combinations

- Vinyl resins based ink systems

- CAP/Acrylic based ink systems

KETJENFLEX® MH is a low molecular weight polymer with extreme low tendency to migrate from the ink or overprint varnish.

Specifications

| Active matter (calcul.): | ≥ 99.5% |
| --- | --- |
| Water content: | 0.5% |
| Softening point: | 55-65oC |
| Acid value: | 0.6 mg KOH/g |
| Colour *): | 40 Pt/Co |
| Turbidity *): | 20 FTU |
| Free formaldehyde: | 0.2% |

*) 25% in butyl acetate

Physical Properties

| Appearance: | hard, transparent resin |
| --- | --- |
| Density: | 1350 kg/m3 |
| Flash point (open cup): | 171oC |
| Boiling point: | decomposes |
| Solubility in water: | practically insoluble |

Toxicological information

| Acute toxicity (oral): | LD50 rat 5000 mg/kg |
| --- | --- |
| Dermal toxicity: | LD50 rat ≥ 7900 mg/kg |
| Acute toxicity (fish, 96h) (Oncorhynchus mykiss) | LC50 ≥ 120 mg/l |
| (Lepomis macrochirus) | LC50 ≥ 130 mg/l |
| Genotoxicity: | not mutagenic |
| Biodegradation: | not readily biodegradable |

KETJENFLEX® MH is approved by the U.S. Food and Drug Administration (FDA) according to CFR  21, section:

- 175.105, 175.300, 175.320, 175.390

- 176.170, 176.180

- 177.1040, limitation: 0.15%

- 177.1200, limitation: 0.6 %

- 177.1400

Packaging

- 10 kg carton board boxes, 100 on a pallet

Storage

Keep packaging well closed. Store in a cool dry place. Elevated temperatures cause the particles to melt together. This has no consequences for the chemical suitability of the product in the final application.